_______________________________________

ARCHITECTURE, ENGINEERING AND CONSTRUCTION

ARCHITECTURE & ENGINEERING

326 East Hoover, Mail Stop B

Ann Arbor, MI  48109-1002

Phone: 734-764-3414

Fax: 734-936-3334

BuildingName
The Description of the Project
P00000000  0000

DOCUMENTS

SPECIFICATION DIVISION  31

NUMBER      SECTION DESCRIPTION

DIVISION 31 EARTHWORK

SECTION 312326 – FLOWABLE FILL

END OF CONTENTS TABLE

DIVISION 31 EARTHWORK

SECTION 312326 – FLOWABLE FILL

GENERAL

THIS SECTION SPECIFIES A PUMPABLE CONCRETE GROUT MATERIAL WITH LIMITED SHRINKAGE - USED IN SPECIAL CIRCUMSTANCES ONLY.

SUMMARY

Work Included:  Class A Compacted Fill as indicated on drawings.

In addition, install embedded items furnished under Division 05 Section "Metal Fabrication".

SUBMITTALS

Submittals:  In addition to product data, submit proposed mix design, including slump and weight data; and copy of laboratory test report showing strengths achieved and expected curing time.

PRODUCTS

ACCEPTABLE MANUFACTURERS

Manufacturer:  Provide materials manufactured by the following:

Flo-Fill Co., 1008 Scheurmann St., Essexville, Mi 48732; phone no. (517)-893-1493.

"Flo-Fill" compacted, class A, fill; complying with the following:

Fly Ash:  approximately 1950 pounds per cubic yard.

Portland cement:  approximately 85 pounds per cubic yard.

Water:  60 to 70 gallons per cubic yard.

Minimum Cured Strength:  6000 pounds per square foot.

Dry Weight:  60 to 70 pounds per cubic foot.

MIXING

Mix material on site in strict accordance with manufacturer's instructions.

EXECUTION

INSTALLATION

Placing:  Pump mixture into place in fluid state to eliminate compaction effort.  Spread and level to grades indicated on drawings.

Curing:  Cure by drying for a minimum of 7 calendar days before placing additional construction over fill material.

END OF SECTION 312326